**CHEMTECH**

***CHEMTECH COATING SOLUTION***

Fact. Add. : S.NO.182/2,Near MESB office,Village-Ware, Tal-Karjat, District-Raigad –410101. Mob:9834094310

E-mail : chemtechcoating@gmail.com

`

***PRODUCT GUIDE***

**COATINGS**

**SR.NO. TRADE DESIGNATIONS & SYSTEM**

**PARTICULARS**

**Resin**

**Hardner**

**Type**

**Ratio**

**Pot life**

**Characterstics & application**

Modified Epoxy Resin /

polyamine System

Solventless rapid systems for primer and self- Levelling flooring and

heavy duty floor coating for high humanity systems

2

3

CER 557

CEH 720

100 : 50 pbw 20 - 30 min.

Solventless, transparent high gloss systems for table top casting

100:35 pbw 90-120 min. and clear coating /Imitation jewellery/ Meena works, Self- Levelling

CER 510

CER 552

CER 551

CEH 7035 - D

CEH 7035 - DR

Modified Epoxy Resin /

polyetheramine System 100:35 pbw

60-90 min Flooring, Protective surface coating, colour retentive, Abrasion

resistant.

Solventless, transparent high gloss systems for Imitation jewellery/

Coating, Self-Levelling, Flooring, Excellent Chemical resistant,

protective surface coatings.

CEH 7050 - DRN CEH 7050 - Modified Epoxy Resin / 100 : 50 pbw

60-90 min

4

5

CLF 559 Clear

CER 552

DN

polyetheramine System 100 : 50 pbw 90-120 min

CEH 735

Modified low viscosity / 100 : 35 pbw 30 - 40 min. Solventless, transparent high gloss systems for Imitation jewellery/

CER 552

CLF 559

Pigmented

Solventless high gloss & highly Chemical resistant coating, Self-

100 : 50 pbw 35 - 45 min. levelling, Floor Topping & surface coating, Abrasion resisrant,

Transparent Imitation Jewellery, colour retentive.

Modified low viscosity /

polyamine System

6

CEH 7963

CEH 7618

CER 552

CLF 559

Pigmented

Solventless high gloss & Chemical resistant coating, Self-levelling,

100 : 50 pbw 35 - 45 min. Floor Topping & surface coating, Abrasion resisrant, Transparent

Imitation Jewellery, colour retentive.

Modified low viscosity /

polyamine System

7

8

Flex Dome

A

Flex Dome

B / Modified / polyamine

System

Flexible, transparent high gloss Systems for doming in Imitation

Jewellery & Label Coatings.

100 : 100 pbw 45 - 60 min.

B - 1

Modified low viscosity

Polyamide

Solventless high solid ambient curing coating & Floorings mainly for

Civil Engineering for Mortar, Screed & Anticorrosive coating .

10

CER 557

CEH 740

100 : 50 pbw 35 - 45 min.

